Build Design

A laser powder bed fusion build was completed on a Colibrium Additive M2 using stainless steel 316H powder. Four types of components were constructed: (1) nominal cylinders, (2) high volumetric energy density (VED) cylinders, (3) spatter generators, and (4) a trigger cylinder. First, 56 nominal cylinders (approximately 15 mm in diameter and 4 in tall) were printed with parameters known from post-build XCT scans to produce material with densities in excess of 99.99%. Next, 8 cylinders with the same dimensions as the nominal cylinders were printed high volumetric energy density (VED) process parameters. All cylinders were designed such that fatigue coupons conforming to ASTM E466 could be excised. Two spatter generation blocks were printed upstream of the cylinders such that they would seed spatter particles across the 64 cylindrical specimens.  Half of the cylinders were located in four rows just downstream of the spatter generators, while the remaining cylinders were placed in four rows not downstream of the spatter generators. Finally, a trigger cylinder was printed to aid with data acquisition stability.

In Situ Sensing

During the construction of the build, two imaging systems were used to collect a total of five images for each layer. First, a 20 MP Basler ace acA5472-17um camera captured images in the post-melt and a post-recoat condition for each layer. Additionally, a 4.2 MP Pixelink PL-D734MU-NIR-T outfitted with a MidOpt Bi808-35.5 filter was used to collect temporally integrated near infrared (TI-NIR) images of each layer. Additional neutral density filters were added to prevent saturation of the detector, and images were collected from the TI-NIR camera at a rate of 5 Hz with an exposure time of 199 ms.

Prior to downstream analysis, data from both the visible light and TI-NIR cameras were preprocessed. Images from the visible light camera were underwent the calibration process outlined in [1] to compensate for non-uniform lighting across the powder bed. Additionally, each frame from the TI-NIR camera was subjected to a custom noise suppression algorithm before all frames corresponding to a single print layer were converted into TI-NIR sum, max, and argmax images by performing pixelwise sum(), max(), and argmax() operations. Both cameras also underwent a calibration procedure to account for intrinsic properties of the lenses responsible for non-linear distortions in the images. Finally, a homographic transformation was applied to the layerwise images from each camera to compensate for their perspective distortions and align the image stack to the build coordinate system. The visible and TI-NIR images had instantaneous fields-of-view of approximately 60 µm and 110 µm, respectively.

Laser scan trajectories were recovered from technical data management streaming (TDMS) files produced by the printer’s QM Meltpool system, which records laser location data and on-axis photodiode signal intensity at approximately 40 kHz. Scan trajectories and associated photodiode signals were then spatially mapped using the methods described in [1], [2].

Anomaly Detection

Process anomalies evident in the layerwise images were detected using a trained instance of the Dynamic Multilabel Segmentation Convolution Neural Network (DMSCNN) described in [3]. The DMSCNN was trained to detect the following anomaly classes:

- Powder: regions of unfused powder within the powder bed.

- Printed: regions of powder fused by the laser beam

- Recoater Hopping: interactions between the recoating mechanism and the powder bed can cause variances in the layer thickness, perpendicular to the travel direction.

- Recoater Streaking: if the recoating mechanism is damaged or dragging a large particle, it can create a streak across the powder bed that changes the effective powder thickness on top of parts

- Incomplete Spreading: occurs if an insufficient amount of powder is dosed across the powder bed

- Powder Mounding: mounds of powder dropped onto the powder bed by the recoater blade

- Debris: these anomalies are typically caused by a delamination or severe warping followed by the recoater striking a part.

- Spatter on Powder: spatter particles ejected from the melt pool and condensed metal vapor can appear as diffuse, dark clouds in the gas flow direction.

- Swelling: certain local geometries (e.g., corners and edges) can cause melt pools to increase in size, distorting the part geometry and allowing it to stick out above the powder layer.

- Super-Elevation: sections of a part sticking up above the powder bed due to either a delamination event or a short feed.

- Misprint: occasionally, a printer will melt an unintended geometry. This can be detected as a misprint by comparing the printed detections to the corresponding *.stl.

- Stripe Boundary: stripe boundaries occur at the intersection between scan blocks. The laser turnarounds at boundaries can change the porosity populations and thermal conditions.

- Over Melting: parts melted with high energy density process parameters that might be more likely to produce keyholing pores.

- Under Melting: parts melted with low energy density process parameters that might be more likely to produce lack of fusion pores.

- Localized Bright Spot: small bright spots in the TI-NIR images thought to correspond to stochastic spatter particles

- Localized Dark Spot: small dark spots in the TI-NIR images, possibly due to topographical changes in the printed surface

- Dropped NIR Data: this is not an anomaly, but an imaging artifact that occurs when an integrated NIR camera system fails to capture one or more frames of data during melting.

- Pitting: small, localized dark regions in the post-recoat images thought to be caused by small perturbations in the recoated powder layer

X-ray Computed Tomography (XCT)

Following completion of the build, a subsection of each cylindrical specimens, roughly corresponding to the gauge section of the machined fatigue coupons, were XCT scanned with a voxel size of 17.8 µm. Volumetric reconstructions were preprocessed through the deep learning pipelines described in [4] to produce high quality XCT scans, and then the XCT data were registered to the build plate coordinate system using the point-to-plane iterative closest point algorithm with random sample consensus [5], [6]. Internal flaws were detected by applying a Laplacian of Gaussian (LoG) kernel to the raw XCT volumes and then thresholding the resulting saliency responses. Flaw voxels detected in the reconstructed XCT volumes were then clustered, and morphological aspects (i.e., size and shape metrics) of each flaw cluster were calculated.

Fatigue Testing

Of the 64 cylinders manufactured, 60 were selected for fatigue testing following XCT scanning. These cylinders were machined into fatigue coupons conforming to ASTM E466 and then subjected to fatigue testing with a stress ratio of 0.1 at 30 Hz. Half of the coupons were tested at a maximum stress level of 300 MPa, which generally falls within the range of high cycle fatigue tests for additively manufactured stainless steels. The other half of the coupons were tested at a maximum stress level of 450 MPA, which corresponds to low cycle fatigue testing.

Thermal Simulations

Melt pool geometry, including the melt pool depth, length, and width, along the scan path was estimated using the methods described in [7], [8], [9], [10] using the components scan trajectories extracted from the TDMS files. This includes scan geometry, raster speed, laser power, and spot size. Material properties for stainless steel 316L used were approximated from temperature-dependent data from Kim [11]. Melt pool dimensions correspond to the dimensions of the melt pool at a given laser position and were calculated by drawing a bounding box around the liquidus isotherm and extracting the corresponding length, width, and depth. Due to the semi-analytical nature of the underlying heat transfer model, a systematic error in the melt pool geometries is expected. Therefore, only relative values and trends should be considered during analyses of these data. Note that only a subset of parts and layers have thermal simulation results.

References

[1]	L. Scime et al., “A Data-Driven Framework for Direct Local Tensile Property Prediction of Laser Powder Bed Fusion Parts,” Materials, vol. 16, no. 23, p. 7293, Nov. 2023, doi: 10.3390/ma16237293.

[2]	W. Halsey, D. Rose, L. Scime, R. Dehoff, and V. Paquit, “Localized Defect Detection from Spatially Mapped, In-Situ Process Data With Machine Learning,” Front. Mech. Eng., vol. 7, p. 767444, Nov. 2021, doi: 10.3389/fmech.2021.767444.

[3]	Z. Snow, L. Scime, A. Ziabari, V. Paquit, and B. Fisher, “Recent Advances on the Use of In Situ Monitoring as a Nondestructive Evaluation Tool for Additive Manufacturing Processes,” in Advancing Precision in Additive Manufacturing, ASPE, Jul. 2024, pp. 86–90.

[4]	A. Ziabari et al., “Enabling rapid X-ray CT characterisation for additive manufacturing using CAD models and deep learning-based reconstruction,” Npj Comput. Mater., vol. 9, no. 1, p. 91, May 2023.

[5]	Y. Chen and G. Medioni, “Object modelling by registration of multiple range images,” Range Image Underst., vol. 10, no. 3, pp. 145–155, Apr. 1992, doi: 10.1016/0262-8856(92)90066-C.

[6]	S. Rusinkiewicz and M. Levoy, “Efficient variants of the ICP algorithm,” in Proceedings Third International Conference on 3-D Digital Imaging and Modeling, Quebec City, Que., Canada: IEEE Comput. Soc, 2001, pp. 145–152. doi: 10.1109/IM.2001.924423.

[7]	B. Stump and A. Plotkowski, “An adaptive integration scheme for heat conduction in additive manufacturing,” Appl. Math. Model., vol. 75, pp. 787–805, Nov. 2019, doi: 10.1016/j.apm.2019.07.008.

[8]	B. Stump, S. Reeve, G. L. Knapp, and B. Cassidy, “3DThesis version 3.0.0.” 2024. doi: https://doi.org/10.5281/zenodo.13686743.

[9]	G. L. Knapp, S. Reeve, J. Coleman, and J. Stump, “ORNL-MDF/Myna: Version 1.0.” 2024. doi: https://doi.org/10.5281/zenodo.13345125.

[10]	G. L. Knapp et al., “Leveraging the digital thread for physics-based prediction of microstructure heterogeneity in additively manufactured parts,” Addit. Manuf., vol. 78, p. 103861, Sep. 2023, doi: 10.1016/j.addma.2023.103861.

[11]	C. Kim, “Thermophysical properties of stainless steels,” Argonne National Laboratory, 1975. [Online]. Available: https://doi.org/10.2172/4152287